## Slide 1: mRaman
Introduction and Applications in Raman Spectroscopy
Aaron Celestian

## Slide 2: Uses of Raman Spectroscopy
Finger printing of compounds
  Crystalline or non-crystalline
  All materials have different Raman spectrums
Fast
  Data can be obtained in less than one second
  Mostly non-destructive
Ease of Use
  “Point-and-Shot” analysis
  No sample preparation
  Laser spot sizes down to 1 micron or less

## Slide 3: Examples
Pigment Analysis
  contact your art department
Compositional Mapping
  Phenocryst zoning analysis
Fluid inclusion analysis
  Presence of N2, CO2, CH4, H2O
  Density of CO2 (European Journal of Mineralogy 2008; DOI: 10.1127/0935-1221/2008/0020-1825)
Monitor mineralogical processes

## Slide 4: Dispersive Raman Microscope
Thermo DXR
Rigakuraman.com

## Slide 5: What information is in the spectrum?
Chart: Raman Shift (cm-1)
External Modes
Rigid units
Internal Modes
Internal polyhedral bonds
Region of External Modes
Internal Modes

## Slide 6: What information is in the spectrum?
Chart: Raman Shift (cm-1)
Characteristic Raman frequencies tell you the composition of the materials.
Look up frequencies in a database
Chemical components
  CO3
  CO2
  SiO4
Pattern of peak positions can identify compound

## Slide 7: What information is in the spectrum?
Chart: Raman Shift (cm-1)
Shifts in peak position:
Stress / strain
Changes in composition can induced stress

## Slide 8: What information is in the spectrum?
Chart: Raman Shift (cm-1)
Width of the peak:
Stress / strain state
  Quality of the crystal – degree of molecular order

## Slide 9: What information is in the spectrum?
Change in intensity can be due to:
Crystal-Laser polarization directions
Amount of material being probed (thickness of sample)
Chart: Raman Shift (cm-1)

## Slide 10: Search and Match
Commercial Software
  Usually comes with the instrument
  Usually have to pay for the databases
  Usually do not contain minerals
CrystalSleuth (Robert Downs)
  Free (http://rruff.info/)
  Contains only minerals
Show search-match
with an ‘unknown 1’
Show search-match
with an ‘unknown 2’

## Slide 11: Zoned Alkali Feldspars
Albite – Anorthite
Elaine Flynn (S) and Andrew Wulff (P) mined data from the RRUFF database
Plot peak position as a function of composition
Data from RRUFF and Freeman et al. (2008) CHARACTERIZATION OF NATURAL FELDSPARS BY RAMAN SPECTROSCOPY FOR FUTURE PLANETARY EXPLORATION
The Canadian Mineralogist
Vol. 46, pp. 1477-1500
DOI : 10.3749/canmin.46.6.1477
Triangles = plag series Squares = Orthoclase
Asterisks = Ternary Feldspars X = unknown

## Slide 12
Data from Bischoff, Sharma, and Mackenzie (1985) American Mineralogist, 70, 581-589

## Slide 13: Tufa Barstow, CA
Organic Layers
Calcite Layers
Crystal Fabrics
Growth Patterns
Trace Minerals
100x
500x

## Slide 14: Raman Map of Crinoid Stem
Darker blues are the stereom and lighter blues, yellows, and reds are the skeletal framework.
Intensity variations in this map just show where there is more calcite than in other areas.
(Dickson slide #107-41)
Skeletal Framework
~3 mol% MgCO3

## Slide 15
~3.0(1) mol% MgCO3
There is a very little difference in the peak position within the ambulacra and outside ambulacra
Extracted line profile from Raman Map
This correlates with the start and stop of the ambulacral grooves (roughly outlined in yellow by hand)
Reflected Light
Close to the center of the channel, there isn’t much change with respect to Mg increase. Only a few mol %.
~2.3(1) mol% MgCO3
~2.3(1) mol% MgCO3

## Slide 16: Ion Exchange
Zeolites and micro-porous molecular
Watch reactions taking place in real time
In Class Exercises:
  Use of various natural and synthetic microporous structures
  Nuclear waste sequestration (Cs and Sr)
  Water softening
  NH4 removal

## Slide 17
Experimental Setup for In Situ Raman Studies

## Slide 18: Time Resolved K  Na-NAT
Time resolved data of K exchange into Na-natrolite. Note the two different exchange steps.
A decrease in peak intensity
Shift in peak position to lower wavenumbers

## Slide 19
This is the Iterative Targeted Transformation Factor Analysis which helps determine when changes are occurring in the spectra.
Students still to do peak fitting and EPE deconvolution.
Intensity
Intensity Shift
Estimated Peak Evolution
Estimated Pure Spectra Based on a Two Component ITTFA
Green = Na-NAT
Blue = K-NAT
Frame number relative to frame 76
X position
Softening of the 8MR
8MR changes to more circular
Home built ITTFA

## Slide 20: Summary of Raman
Non destructive
Fast
Little to no sample preparation
Experiments to accompany structural studies
Leaves students with a new tool and encourage undergraduate research